[image: image1.jpg]COOPERATIVA DE TRABAJO,
ROSETTASTONELTDA





1.1.1 Scope of Refractory Repair

The description of the individual work is under item 4:

· Oven sole

· Oven roof

· Uncaulking and Caulking of the door frames

· Cleaning of the regenerators for 2 flues deep

· Adjustment / Alignment of the heating wall face

· Instalation of door plugs in new doors and demolition of refractory parts in old doors

Note: Items, which have to be inserted into / attached to the refractory brickwork, such as ceramic fiber mats between wall protection plate and brickwork, charging hole frames, inspection hole frames, ascension pipe base sleeves, goose neck, charging car rail chairs, etc. are to be installed by the contractor of the refractory works (during bricklaying). However, sealing and caulking is part of this specification.
1.1.2 Physical condition of the batteries

Before start of the execution of each individual repair step a joint inspection by Company 1, Company 2 and CONTRACTOR shall be carried out in order to verify the scheduled scope of revamping and to determine other necessities of maintenance and/or repair during the execution. The inspection shall comprise:

· Inspection of the chamber walls and oven roof for

· deformation and/or bulges

· spalling and molten areas

· crack formation and open joints

· condition of areas previously repaired

· water ingress

· condition of oven sole

· Inspection of all heating flues for

· clogged or choked rich gas nozzles

· deposits on burner level or clogged air ports

· leakage or raw gas transfer into the heating flues

· visual evaluation of the combustion based on the flame profile

· checking of the regenerator checker bricks on deposits or clogging by means of measurement of pressure conditions and, as a result of these measurements, visually, if required.


[image: image1.jpg]